## Slide 1: d6_LHS_b3

## Slide 2: Room temperature pulses
Room temp behaviour as it should be.
Just Joule heating from pulses. Background change in resistance is due to temperature drift (not actually including this figure in a paper due to the background drift. Included some nicer data from another device).
Overall variation due to temp changes

## Slide 3: RvT4
Heating after applying pulses
Region 0: 0-2500s
Ramp up the temperature from 320-404K

## Slide 4: RvT4
Odd behaviour in this region. Appear to be flicking down to a new state but it’s slightly different for positive and negative pulses
106 pulse train. Surrounding areas are 105 (see next slide)
Much more mixed behaviour in this region

## Slide 5: RvT4
N=10^5
Pulses:
All pulses marked are trains of N
1us pulses with 9us recovery time.
Delay between pulse trains is 120 seconds.
N=10^6
N=10^5
N=10^3
N=10^4

## Slide 6: RvT5
Mixture of applying pulses and temperature changes
The first pulse at a new temperature appears to move transition in line with cooling branch.
On increasing the temperature the state then moves back towards the heating branch.
Can see these points on the R vs time plot.
Also see cooling branch matches up well with an earlier measurement

## Slide 7: R v Temp
Cooling arm is reliably the same shape.
Heating arm varies between temperature cycles

## Slide 8: RvT8
Back to 404K
Mixed behaviour from pulses
Can see behaviour is the same as in RvT2
All positive pulses do the same as all negative pulses
For positive pulses in a row and negative the pulse amp is 40mA and its 1e-6,9e-6, 1e6 pulses.